## Slide 1
St. Joseph’s College of Engineering and Technology, Thanjavur
Department of Mechanical Engineering
Material Selection for a Quadcopter Drone Arm Using Beam Theory and TOPSIS Method
Track: Propulsion and Structures
Dr. S. R. Sathishkumar, [Staff Name]
[Student 1], [Student 2], [Student 3], [Student 4]
ICAAN–2026 · Saranathan College of Engineering, Tiruchirappalli · 15–16 October 2026
Notes: Presenter 1: Greet, introduce the team, read the title. One line: we found the best material for a drone arm using simple strength-of-materials formulas and a ranking method called TOPSIS.

## Slide 2: Why does the drone arm material matter?
The arm holds the motor and carries its thrust to the frame
Heavy arm → shorter flight time (battery limited)
Flexible arm → vibration and poor control
Weak arm → breaks in a hard landing
So we need: light + stiff + strong + affordable
Arm
Motor
450 mm quadcopter (X-frame)
Notes: Presenter 1: Point to the drawing. Each of the four arms holds a motor. A heavy arm reduces flight time, a bendy arm vibrates, a weak arm breaks. We want the best balance.

## Slide 3: Objectives
1
Model the drone arm as a cantilever beam and find its stress and deflection
2
Compare five materials for mass, deflection, factor of safety and cost
3
Rank the materials with the TOPSIS method and check the effect of weights
Notes: Presenter 1: Three steps – calculate, compare, rank.

## Slide 4: Arm modelled as a cantilever beam
Frame (fixed)
F = 20 N
L = 200 mm
Tube cross-section:
D = 12 mm, d = 10 mm
Design data
Drone: 450 mm, ≈ 1.5 kg
Max motor thrust: 10 N
Safety factor: 2
Design load F = 10 × 2 = 20 N
Load at free end (motor)
Notes: Presenter 2: The arm is fixed at the frame and the motor pushes up at the other end – exactly a cantilever from Strength of Materials. The motor gives up to 10 N; we double it for safety, so 20 N.

## Slide 5: Calculation using beam theory
Moment of inertia
I = π(D⁴ − d⁴)/64
527.0 mm⁴
Section modulus
Z = I / (D/2)
87.8 mm³
Bending moment
M = F × L = 20 × 200
4000 N·mm
Bending stress
σ = M / Z
45.5 MPa
Tip deflection
δ = F L³ / (3 E I)
depends on E
Mass
m = ρ × A × L
depends on ρ
Notes: Presenter 2: These are textbook formulas. Same tube shape for all materials, so the stress is the same 45.5 MPa for all. Deflection changes with E (stiffness) and mass changes with density. You can work these on a calculator.

## Slide 6: Candidate materials
Material | Density (kg/m³) | E (GPa) | Strength (MPa) | Cost (₹/kg, approx.)
Steel AISI 4130 | 7850 | 205 | 460 | 250
Aluminium 6061-T6 | 2700 | 69 | 276 | 350
Titanium Ti-6Al-4V | 4430 | 114 | 880 | 3,500
GFRP (glass/epoxy) | 1900 | 25 | 350 | 700
CFRP (carbon/epoxy) | 1600 | 70 | 600 | 3,000
Source: typical handbook values (ASM Handbook, MatWeb). Strength = yield for metals, tensile for composites. Costs are approximate Indian market prices, used only for comparison.
Notes: Presenter 2: Two metals commonly used, one premium metal (titanium) and two composites. Values come from standard handbooks.

## Slide 7: Results: arm mass and tip deflection
Chart: Arm mass (g)
| Steel 4130 | Al 6061-T6 | Ti-6Al-4V | GFRP | CFRP
Arm mass (g) | 54.3 | 18.7 | 30.6 | 13.1 | 11.1
Chart: Tip deflection (mm)
| Steel 4130 | Al 6061-T6 | Ti-6Al-4V | GFRP | CFRP
Tip deflection (mm) | 0.49 | 1.47 | 0.89 | 4.05 | 1.45
CFRP is lightest (11.1 g, ~80% lighter than steel); steel is stiffest but 5× heavier; GFRP bends the most
Notes: Presenter 3: Left – weight. Carbon fibre is the lightest. Right – how much the tip bends. Steel bends least but is very heavy. Glass fibre bends 4 mm, which is too flexible.

## Slide 8: Results: factor of safety and cost
Chart: Factor of safety
| Steel 4130 | Al 6061-T6 | Ti-6Al-4V | GFRP | CFRP
Factor of safety | 10.1 | 6.1 | 19.3 | 7.7 | 13.2
Chart: Material cost per arm (₹)
| Steel 4130 | Al 6061-T6 | Ti-6Al-4V | GFRP | CFRP
Material cost per arm (₹) | 13.6 | 6.5 | 107.2 | 9.2 | 33.2
All materials are safe (FoS > 6); titanium is strongest but costliest; aluminium is cheapest
Notes: Presenter 3: Every material is safe – factor of safety above 6. So the choice depends on weight, stiffness and cost. That is why we need a ranking method.

## Slide 9: TOPSIS ranking method in 6 steps
1
Decision matrix
Materials × criteria table
2
Normalise
Divide by √(sum of squares)
3
Apply weights
Mass 0.35, Deflection 0.25, FoS 0.20, Cost 0.20
4
Ideal best & worst
Best and worst value of each criterion
5
Distances
D+ to best, D− to worst
6
Closeness score
C = D− / (D+ + D−); highest = best
TOPSIS = Technique for Order of Preference by Similarity to Ideal Solution
Notes: Presenter 4: TOPSIS picks the option closest to an imaginary perfect material and farthest from the worst one. All steps are simple arithmetic and are shown in our Excel sheet.

## Slide 10: TOPSIS result: CFRP ranks first
Chart: Closeness score C (higher = better)
| CFRP | Al 6061-T6 | GFRP | Ti-6Al-4V | Steel 4130
Closeness score | 0.784 | 0.713 | 0.568 | 0.529 | 0.519
1st CFRP
Lightest, stiff and very safe – best overall
2nd Aluminium 6061-T6
Cheapest and easy to machine – best budget choice
Notes: Presenter 4: Carbon fibre scores 0.784 and comes first; aluminium is second with 0.713. Steel is last because it is too heavy.

## Slide 11: Does the result change with weights?
Base weights
Mass 0.35 · Defl. 0.25 · FoS 0.20 · Cost 0.20
Rank 1: CFRP
Equal weights
0.25 each
Rank 1: CFRP
Cost-focused
Mass 0.25 · Defl. 0.15 · FoS 0.15 · Cost 0.45
Rank 1: Aluminium 6061-T6
Matches real practice: premium drones use carbon-fibre arms, low-cost drones use aluminium arms
Notes: Presenter 4: If we care most about performance, carbon fibre wins. If cost is the main concern, aluminium wins. This matches what we see in the market.

## Slide 12: Conclusion and future work
Conclusion
Bending stress in the arm is only 45.5 MPa – all five materials are safe
CFRP is the best overall choice (C = 0.784, 11.1 g arm)
Aluminium 6061-T6 is the best low-cost choice
Simple beam theory + TOPSIS gives a quick, transparent decision
Future work
Verify stress and deflection with FEA (ANSYS)
Include vibration (natural frequency) and impact load
Test 3D-printed and natural-fibre composite arms
Notes: Presenter 1: Summarise. Next we will check the results with ANSYS and add vibration and crash loads.

## Slide 13: References
R. C. Hibbeler, Mechanics of Materials, 10th ed., Pearson, 2017.
M. F. Ashby, Materials Selection in Mechanical Design, 5th ed., Butterworth-Heinemann, 2017.
C. L. Hwang and K. Yoon, Multiple Attribute Decision Making: Methods and Applications, Springer, 1981.
ASM International, ASM Handbook, Vol. 2: Properties and Selection – Nonferrous Alloys, 1990.
MatWeb Material Property Data, www.matweb.com (accessed October 2026).

## Slide 14
Thank you
Questions?
Department of Mechanical Engineering, St. Joseph’s College of Engineering and Technology, Thanjavur